| טיוטה לתקן ישראלי ת"י 597 חלק 1 | Draft SI 597 part 1 |
| --- | --- |
| יוני 2015 | june 2015 |
|  | ICS CODE: - |

צמר גפן סופג

Absorbent cotton wool

תקן זה הוכן על ידי הוועדה הטכנית

ריכז את עבודת הכנת התקן.

הודעה על רוויזיה

תקן ישראלי זה בא במקום התקן הישראלי ת"י 597

מילות מפתח:

Descriptors:

עדכניות התקן

התקנים הישראליים עומדים לבדיקה מזמן לזמן, ולפחות אחת לחמש שנים, כדי להתאימם להתפתחות המדע והטכנולוגיה.

המשתמשים בתקנים יוודאו שבידיהם המהדורה המעודכנת של התקן על גיליונות התיקון שלו.

מסמך המתפרסם ברשומות כגיליון תיקון, יכול להיות גיליון תיקון נפרד או תיקון המשולב בתקן.

תוקף התקן

תקן ישראלי על עדכוניו נכנס לתוקף החל ממועד פרסומו ברשומות.

יש לבדוק אם התקן רשמי או אם חלקים ממנו רשמיים. תקן רשמי או גיליון תיקון רשמי (במלואם או בחלקם) נכנסים לתוקף

60 יום מפרסום ההודעה ברשומות, אלא אם בהודעה נקבע מועד מאוחר יותר לכניסה לתוקף.

סימון בתו תקן

כל המייצר מוצר, המתאים לדרישות התקנים הישראליים החלים עליו,

רשאי, לפי היתר ממכון התקנים הישראלי, לסמנו בתו תקן:

זכויות יוצרים

( אין לצלם, להעתיק או לפרסם, בכל אמצעי שהוא, תקן זה או קטעים ממנו, ללא רשות מראש ובכתב ממכון התקנים הישראלי.

הקדמה לתקן הישראלי

תקן ישראלי זה הוא מונוגרף הפרמקופיאה האירופית Ph Eur monograph 0036 – Absorbent Cotton שאושר           כתקן ישראלי בשינויים ובתוספות לאומיים.

או

תקן ישראלי זה הוא מונוגרף הפרמקופיאה האמריקנית USP Purified cotton שאושר  כתקן ישראלי בשינויים ובתוספות לאומיים.

הערה:

התקן הישראלי מאפשר בחירה בין שני מסלולי אימוץ: אימוץ מונוגרף הפרמקופיאה האירופית או אימוץ מונוגרף הפרמקופיאה האמריקנית, לרבות השינויים והתוספות הלאומיים.

לא ניתן לשלב בין שני מסלולי האימוץ, ויש להיצמד למסלול הנבחר במלואו.

התקן כולל, בסדר המפורט להלן, רכיבים אלה:

- מסלול אימוץ מונוגרף הפרמקופיאה האירופית

- חלות (בעברית)

- פירוט השינויים והתוספות הלאומיים לסעיפי מונוגרף הפרמקופיאה האירופית (בעברית)

- מונוגרף הפרמקופיאה האירופית Ph Eur monograph 0036 – Absorbent Cotton (באנגלית)

- - מסלול אימוץ מונוגרף הפרמקופיאה האמריקאית

- - חלות (בעברית)

- - פירוט השינויים והתוספות הלאומיים לסעיפי מונוגרף הפרמקופיאה האמריקנית (בעברית)

- - מונוגרף הפרמקופיאה האמריקנית USP Purified cotton (באנגלית)

תקן זה הוא חלק מסדרת תקנים החלה על צמר גפן ותחליפיו.

חלקי הסדרה הם אלה:

ת"י 597 חלק 1  -  צמר גפן

ת"י 597 חלק 2  -  תחליף צמר גפן

# מסלול אימוץ הפרמקופיאה האירופית Ph Eur monograph 0036 – Absorbent Cotton

## חלות התקן

תקן זה חל על צמר גפן (להלן: המוצר) לשימוש רפואי ולשימוש קוסמטי.

תקן זה אינו חל על מקלות לניקוי אוזניים ועל צמר גפן לשימוש דנטלי.

פירוט השינויים והתוספות הלאומיים לסעיפי מונוגרף הפרמקופיאה האירופית

Ph Eur monograph 0036 – Absorbent Cotton

בסעיף Charecters במקום המילים "determined by a suitable method" ייכתב "בודקים כמפורט בתקן של האגודה האמריקנית לבדיקות ולחומרים ASTM D 1440".

לפני סעיף storage יוסף סעיף אריזה וסימון, כמפורט להלן:

## אריזה וסימון

### אריזה

צמר גפן המסופק בצורה רציפה מגוללת יהודק בחבילה כך שיהיה אפשר לצבוט ממנו במשיכה בכוח סביר.

### סימון

המוצר יסומן בשפה העברית ויכלול פרטים אלה:

- כינוי המוצר ( לדוגמה: צמר גפן – שכבה רציפה, צמר גפן – שכבה רציפה בעלת נקבים לתלישה,    צמר גפן – שכבה רציפה מגוללת, צמר גפן – כדורים, צמר גפן – דסקיות ("פדים"), וכד')

- שם היצרן, באותיות שגובהן 3 מ"מ לפחות, וסימן המסחר הרשום שלו (אם קיים). 
אם המוצר מיובא, יסומנו שם היבואן, כתובתו וארץ הייצור, באותיות שגובהן 3 מ"מ לפחות;

- תאריך הייצור – חודש ושנה, או סימון אחר לזיהוי מנת הייצור;

- משקל יחידת האריזה (ג').

- אם המוצר מעוקר, המילה "מעוקר"

באריזות המכילות כמה יחידות אריזה יחד יסומן על האריזה מספר יחידות האריזה.

לאחר סעיף storage יוסף סעיף בדיקות מיקרוביולוגיות כמפורט להלן:

בדיקות מיקרוביולוגיות

בודקים בבדיקה זו מוצרים לא מעוקרים(1) .

בודקים את המוצר כמפורט בפרמקופיאה האירופית (מהדורה 7), על עדכוניה, בפרק 2.6.12 הדן בספירת מושבות:

2.6.12 	microbiological examination of non-sterile products: total viable aerobic count

ובפרק 2.6.13 הדן בבדיקה לאיתור מיקרואורגניזמים נקובים:

2.6.13 	microbiological examination of non-sterile products: test for specified micro-organisms

המוצר יעמוד בדרישות המפורטות בסעיף 5.1.4 בפרמקופיאה האירופית (מהדורה 7), על עדכוניה, למוצרים המיועדים לשימוש על העור:

5.1.4 	microbiological quality of non-sterile pharmaceutical preparations and substances for

pharmaceutical use

מסלול אימוץ הפרמקופיאה האמריקאית

## חלות התקן

תקן זה חל על צמר גפן (להלן: המוצר) לשימוש רפואי ולשימוש קוסמטי.

תקן זה אינו חל על מקלות לניקוי אוזניים ועל צמר גפן לשימוש דנטלי.

פירוט השינויים והתוספות הלאומיים לסעיפי מונוגרף הפרמקופיאה האמריקנית

USP Purified cotton

בסעיף Purified cotton המילים "and sterilized in its final container" אינן חלות

לפני סעיף storage יוסף סעיף אריזה וסימון, כמפורט להלן:

## אריזה וסימון

### אריזה

צמר גפן המסופק בצורה רציפה מגוללת יהודק בחבילה כך שיהיה אפשר לצבוט ממנו במשיכה בכוח סביר.

### סימון

המוצר יסומן בשפה העברית ויכלול פרטים אלה:

- כינוי המוצר ( לדוגמה: צמר גפן – שכבה רציפה, צמר גפן – שכבה רציפה בעלת נקבים לתלישה,    צמר גפן – שכבה רציפה מגוללת, צמר גפן – כדורים, צמר גפן – דסקיות ("פדים"), וכד')

- שם היצרן, באותיות שגובהן 3 מ"מ לפחות, וסימן המסחר הרשום שלו (אם קיים). 
אם המוצר מיובא, יסומנו שם היבואן, כתובתו וארץ הייצור, באותיות שגובהן 3 מ"מ לפחות;

- תאריך הייצור – חודש ושנה, או סימון אחר לזיהוי מנת הייצור;

- משקל יחידת האריזה (ג').

- אם המוצר מעוקר, המילה "מעוקר"

באריזות המכילות כמה יחידות אריזה יחד יסומן על האריזה מספר יחידות האריזה.

לאחר סעיף  אריזה וסימון ייכתב דרישות עבור מוצר המסומן "מעוקר"

הכתוב בסעיף Sterility יושמט ובמקומו ייכתב:

מוצר המסומן "מעוקר" יעמוד בקריטריונים המפורטים בתקן הישראלי ת"י 4151

לפני סעיף Acidity or alkalinity ייכתב דרישות עבור מוצר המסומן "מעוקר" ועבור מוצר שאינו מסומן "מעוקר"

לאחר סעיף Residual solvents יוסף סעיף בדיקות מיקרוביולוגיות, כמפורט להלן:

בדיקות מיקרוביולוגיות

בודקים בבדיקה זו מוצרים לא מעוקרים1) .

בודקים את המוצר כמפורט בפרמקופיאה האמריקאית, על עדכוניה, בפרק <61>הדן בספירת מושבות:

2.6.12 	microbiological examination of non-sterile products: total viable aerobic count

ובפרק <62>הדן בבדיקה לאיתור מיקרואורגניזמים נקובים:

2.6.13 	microbiological examination of non-sterile products: test for specified micro-organisms

המוצר יעמוד בדרישות המפורטות בסעיף <1111> בפרמקופיאה האמריקאית , על עדכוניה, למוצרים המיועדים לשימוש על העור:

<1111>   MICROBIOLOGICAL EXAMINATION OF NONSTERILE PRODUCTS: ACCEPTANCE CRITERIA FOR PHARMACEUTICAL PREPARATIONS AND SUBSTANCES FOR PHARMACEUTICAL USE

Absorbent Cotton

(Ph Eur monograph 0036)

Ph Eur

Definition

Absorbent cotton consists of new fibres or good quality combers obtained from the seed-coat of various species of the genus Gossypium L., cleaned, purified, bleached and carefully carded. It may not contain any compensatory colouring matter.

Characters

It is white and is composed of fibres of average length not less than 10 mm, determined by a suitable method, and contains not more than traces of leaf residue, pericarp, seed-coat or other impurities. It offers appreciable resistance when pulled. It does not shed any appreciable quantity of dust when gently shaken.

Identification

A.	Examined under a microscope, each fibre is seen to consist of a single cell, up to about 4 cm long and up to 40 mm wide, in the form of a flattened tube with thick and rounded walls and often twisted.

B.	When treated with iodinated zinc chloride solution R, the fibres become violet.

C.	To 0.1 g add 10 ml of zinc chloride-formic acid solution R. Heat to 40C and allow to stand for 2 h 30 min, shaking occasionally. It does not dissolve.

Tests

Solution S

Place 15.0 g in a suitable vessel, add 150 ml of water  R, close the vessel and allow to macerate for 2 h. Decant the solution, squeeze the residual liquid carefully from the sample with a glass rod and mix. Reserve 10 ml of the solution for the test for surface-active substances and filter the remainder.

Acidity or alkalinity

To 25 ml of solution S add 0.1 ml of phenolphthalein solution R and to another 25 ml add 0.05 ml of methyl orange solution R. Neither solution is pink.

Foreign fibres

Examined under a microscope, it is seen to consist exclusively of typical cotton fibres, except that occasionally a few isolated foreign fibres may be present.

Fluorescence

Examine a layer about 5 mm in thickness under ultraviolet light at 365 nm. It displays only a slight brownish-violet fluorescence and a few yellow particles. It shows no intense blue fluorescence, apart from that which may be shown by a few isolated fibres.

Neps

Spread about 1 g evenly between 2 colourless transparent plates each 10 cm square. Examine for neps by transmitted light and compare with Absorbent cotton RM. The product to be examined is not more neppy than the standard.

Absorbency

Apparatus

A dry cylindrical copper wire basket 8.0 cm high and 5.0 cm in diameter. The wire of which the basket is constructed is about 0.4 mm in diameter, the mesh is 1.5 cm to 2.0 cm wide and the mass of the basket is 2.7 g 0.3 g.

Sinking time

Not more than 10 s. Weigh the basket to the nearest centigram (m1). Take a total of 5.00 g in approximately equal quantities from 5 different places in the product to be examined, place loosely in the basket and weigh the filled basket to the nearest centigram (m2). Fill a beaker 11 cm to 12 cm in diameter to a depth of 10 cm with water at about 20C. Hold the basket horizontally and drop it from a height of about 10 mm into the water. Measure with a stopwatch the time taken for the basket to sink below the surface of the water. Calculate the result as the average of 3 tests.

Water-holding capacity

Not less than 23.0 g of water per gram. After the sinking time has been measured, remove the basket from the water, allow it to drain for exactly 30 s suspended in a horizontal position over the beaker, transfer it to a tared beaker (m3) and weigh to the nearest centigram (m4). Calculate the water-holding capacity per gram of absorbent cotton using the following expression:

Calculate the result as the average of 3 tests.

Ether-soluble substances

Not more than 0.50 per cent. In an extraction apparatus, extract 5.00 g with ether  R for 4 h at a rate of at least 4 extractions per hour. Evaporate the ether extract and dry the residue to constant mass at 100C to 105C.

Extractable colouring matter

In a narrow percolator, slowly extract 10.0 g with alcohol  R until 50 ml of extract is obtained. The liquid obtained is not more intensely coloured (2.2.2, Method II) than reference solution Y5, GY6 or a reference solution prepared as follows: to 3.0 ml of blue primary solution add 7.0 ml of hydrochloric acid (10 g/l HCl). Dilute 0.5 ml of this solution to 10.0 ml with hydrochloric acid (10 g/l HCl).

Surface-active substances

Introduce the 10 ml portion of solution S reserved before filtration into a 25 ml graduated ground-glass-stoppered cylinder with an external diameter of 20 mm and a wall thickness of not greater than 1.5 mm, previously rinsed 3 times with sulphuric acid R and then with water  R. Shake vigorously 30 times in 10 s, allow to stand for 1 min and repeat the shaking. After 5 min, any foam present must not cover the entire surface of the liquid.

Water-soluble substances

Not more than 0.50 per cent. Boil 5.000 g in 500 ml of water  R for 30 min, stirring frequently. Replace the water lost by evaporation. Decant the liquid, squeeze the residual liquid carefully from the sample with a glass rod and mix. Filter the liquid whilst hot. Evaporate 400 ml of the filtrate (corresponding to 4/5 of the mass of the sample taken) and dry the residue to constant mass at 100C to 105C.

Loss on drying (2.2.32)

Not more than 8.0 per cent, determined on 5.000 g by drying in an oven at 100C to 105C.

Sulphated ash (2.4.14)

Not more than 0.40 per cent. Introduce 5.00 g into a previously heated and cooled, tared crucible. Heat cautiously over a naked flame and then carefully to dull redness at 600C. Allow to cool, add a few drops of dilute sulphuric acid R, then heat and incinerate until all the black particles have disappeared. Allow to cool. Add a few drops of ammonium carbonate solution R. Evaporate and incinerate carefully, allow to cool and weigh again. Repeat the incineration for periods of 5 min to constant mass.

Storage

Store in a dust-proof package in a dry place.

Ph Eur

Purified Cotton

» Purified Cotton is the hair of the seed of cultivated varieties of Gossypium hirsutum Linnי, or of other

species of Gossypium (Fam. Malvaceae), freed from adhering impurities, deprived of fatty matter,

bleached, and sterilized in its final container.

Packaging and storage— Package it in rolls of not more than 500 g of a continuous lap, with a light-weight paper running

under the entire lap, the paper being of such width that it may be folded over the edges of the lap to a distance of at least

25 mm, the two together being tightly and evenly rolled, and enclosed and sealed in a well-closed container. It may be

packaged also in other types of containers if these are so constructed that the sterility of the product is maintained.

Labeling— Its label bears a statement to the effect that the sterility cannot be guaranteed if the package bears evidence of

damage or if the package has been opened previously.

Sterility 71 : meets the requirements.

Acidity or alkalinity— Thoroughly saturate about 10 g with 100 mL of recently boiled and cooled water, then with the aid

of a glass rod press out two 25-mL portions of the water into white porcelain dishes. To one portion add 3 drops of

phenolphthalein TS, and to the other portion add 1 drop of methyl orange TS: no pink color develops in either portion.

Residue on ignition 281 — Place about 5 g, accurately weighed, in a porcelain or platinum dish, and moisten with 2 N

sulfuric acid. Gently heat the cotton until it is charred, then ignite more strongly until the carbon is completely consumed:

not more than 0.20% of residue remains.

Water-soluble substances— Place 10 g, accurately weighed, in a beaker containing 1000 mL of water, and boil gently for

30 minutes, adding water as required to maintain the volume. Pour the water through a funnel into another vessel, and

press out the excess water from the cotton with a glass rod. Wash the cotton in the funnel with two 250-mL portions of

boiling water, pressing the cotton after each washing. Filter the combined extract and washings, and wash the filter

thoroughly with hot water. Evaporate the combined extract and washings to a small volume, transfer to a tared porcelain or

platinum dish, evaporate to dryness, and dry the residue at 105 to constant weight: the residue weighs not more than 35

mg (0.35%).

Fatty matter— Pack 10 ± 0.01 g in a Soxhlet extractor provided with a tared receiver, and extract with ether for 5 hours at

a rate such that the ether siphons over not less than four times per hour. The ether solution in the flask shows no trace of

blue, green, or brownish color. Evaporate the extract to dryness, and dry at 105 for 1 hour: the weight of the residue does

not exceed 70 mg (0.7

Dyes— Pack about 10 g in a narrow percolator, and extract slowly with alcohol until the percolate measures 50 mL: when

observed downward through a column 20 cm in depth, the percolate may show a yellowish color, but neither a blue nor a

green tint.

Other foreign matter— The pinches of it taken for the determination of Fiber length contain no oil stains or metallic

particles.

Fiber length and Absorbency— Remove it from its wrappings, and condition it for not less than 4 hours in a standard

atmosphere of 65 ± 2% relative humidity at 21 ± 1.1 (70 ± 2 F), before determining the Fiber length and Absorbency.

Fiber length— Determine the fiber length of Purified Cotton as directed under Cotton—Fiber Length 691 : not less than

60% of the fibers, by weight, are 12.5 mm or greater in length, and not more than 10% of the fibers, by weight, are 6.25 mm

or less in length.

Absorbency— Proceed as directed under Cotton—Absorbency Test 691 : submersion is complete in 10 seconds at a

temperature of 25 , and the cotton retains not less than 24 times its weight of water.

Residual solvents 467 : meets the requirements.

(Official January 1, 2007)

Auxiliary Information— Staff Liaison : Radhakrishna S Tirumalai, Scientist

Expert Committee : (GTMDB05) General Toxicology and Medical Device Biocompatibility

USP29–NF24 Page 597

Phone Number : 1-301-816-8339

# Footnotes

(1) 	קריטריונים עבור מוצרים המסומנים "מעוקר" מפורטים בתקן הישראלי ת"י 4151.

# Text boxes

מסמך זה הוא הצעה בלבד